## Slide 1: X-Ray Diffraction
Dr. Ranjit Kumar
Department of Chemical Engineering
Email: ranjit.kumar@snu.edu.in

## Slide 2: X-Ray Analysis
X-rays discovered in 1895
Fundamental to understanding of crystal structure and symmetry
Powder diffraction analyses are a simple and inexpensive method for identifying minerals, especially fine-grained minerals

## Slide 3: XRD practical aspects
How do we measure the X‐ray diffraction pattern of a solid?
Powder diffractometer
Sample holder
Detector
Electron gun

## Slide 4: XRD basic theory
The periodic lattice found in crystalline structures may act as a diffraction grating for wave‐ particles or electromagnetic radiation with wavelengths of a similar order of magnitude (10‐10 m or 1 Å).
For solids, there are three particles/waves with wavelengths equivalent to interatomic distances and, hence, which will interact with a specimen as they pass through it: X‐rays, electrons, and neutrons.
When will diffraction occur?
X‐rays, electrons, neutrons
Diffraction
Sample
Detector
I0
It
I0 =>It  transmittance
I0 =>It  diffraction and/or absorbance
Sample
1 Å

## Slide 5: XRD basic theory
Incident radiation
“Reflected” radiation
d
Transmitted radiation
θ
λ
θ
In materials with a crystalline structure, X‐rays scattered by ordered features will be scattered coherently “in‐phase” in certain directions meeting the criteria for constructive interference  signal amplification.
The conditions required for constructive interference are determined by Bragg's law.
Bragg’s Law
n λ = 2d sinθ
λ = X‐ray wavelength
d = distance between lattice planes
θ = angle of incidence with lattice plane
n = integer

## Slide 6: XRD basic theory
What type of materials can we study? Gas: No structural order – see nothing.
Liquid/Amorphous solids: Order over a few angstroms – broad diffraction peaks
Ordered solids: Extensive structural order – sharp diffraction peaks. Two types of ordered solids:
1) Single crystals
2) Polycrystalline powders
Large crystal required. Crystal orientation known.
 Each lattice plane only present in one orientation.
 No overlap of reflections.
 Reflection intensities may be accurately measured.
Most common in heterogeneous catalysis. Assume all crystal orientations present.
 Each lattice plane present at all orientations.
 Many overlapping peaks.
 Reflection intensities are difficult to determine.
18

## Slide 7: XRD basic theory
What determines the intensity of the diffraction peak?
Electron density
X‐rays scattered by electrons
 Greater the atomic number, Z, the higher the scattering factor of a given element (directly proportional).
 Intensity proportional to sum of the scattering factors of atoms in a given lattice plane. I ∝ |F|2
Multiplicity
For Powder samples all planes with equivalent d‐spacing overlap.
 Intensity dependent on number of overlapping planes.

## Slide 8: XRD basic theory
How can we satisfy the Bragg equation?
Bragg’s Law: nλ = 2dsinθ
To observe diffraction from a given lattice plane, Bragg’s law may be satisfied by varying either the wavelength, , or the Bragg angle, .
Monochromatic diffraction:
 Vary 
 Bragg condition met once at a time.
With a fixed wavelength (laboratory source) data is collected as a function of increasing diffraction angle up to a given value of d (resolution dependent).
Laue diffraction:
 Vary .
 Bragg condition met many times simultaneously.
 Faster but greater complexity in data analysis.
 Requires synchrotron which is expensive.

## Slide 9
Interplanar spacing
Bragg’s Equation

## Slide 10
nλ = dhkl sinθ + dhklsinθ
= 2dhkl sinθ
Where,
n = an integer, order of reflection
= 1 (unless stated otherwise)
Bragg’s law of diffraction
nλ =
Bragg’s Equation

## Slide 11
For cubic system,
a2/d2 = h2 + k2 + l2
X-Ray Diffraction
nλ =
= path difference where n = integer = 1
= dhkl sinθ + dhklsinθ
= 2dhkl sinθ
a2/d2 = h2 + k2 + l2

## Slide 12
λ = 2 d sinθ a2/d2 = h2 + k2 + l2
λ = (2 a sinθ)/ √ (h2 + k2 + l2)
sin2θ = λ2(h2 + k2 + l2)/4a2
“ λ” and “a” are constants
Bragg’s Equation

## Slide 13
Problem:
Given: {211} Planes
aFe = 0.2866 nm (2.866Å)
λ = 0.1542 nm (1.542Å)
Determine dhkl, 2θ (diffraction angle)
n = 1
  dhkl = a/ √ (h2 + k2 + l2)
= 0.2866 nm /√ (22 + 12 + 12)
= 0.1170 nm (1.170Å)
  n =1
sinθ = n λ/2dhkl =
θ = sin-1(0.659) = 41.22°
2θ = 82.44°

## Slide 14
Relationship between d‐spacing and lattice constants
System
dhkl
Cubic
Tetragonal
Orthorhombic
Hexagonal Rhombohedral
Monoclinic
Triclinic
 Increasingly complex with decreasing symmetry.
 Simplest for orthogonal crystal systems

## Slide 16
Bravais Lattice | Reflections which may be present | Reflections necessarily absent
Simple | all | None
Body centred | (h + k + l) even | (h + k + l) odd
Face centred | h, k and l unmixed | h, k and l mixed
End centred | h and k unmixed C centred | h and k mixed C centred
Bravais Lattice | Allowed Reflections
SC | All
BCC | (h + k + l) even
FCC | h, k and l unmixed
DC | h, k and l are all odd Or all are even & (h + k + l) divisible by 4
Selection / Extinction Rules

## Slide 17
h2 + k2 + l2 | SC | FCC | BCC | DC
1 | 100 |  |  | 
2 | 110 |  | 110 | 
3 | 111 | 111 |  | 111
4 | 200 | 200 | 200 | 
5 | 210 |  |  | 
6 | 211 |  | 211 | 
7 |  |  |  | 
8 | 220 | 220 | 220 | 220
9 | 300, 221 |  |  | 
10 | 310 |  | 310 | 
11 | 311 | 311 |  | 311
12 | 222 | 222 | 222 | 
13 | 320 |  |  | 
14 | 321 |  | 321 | 
15 |  |  |  | 
16 | 400 | 400 | 400 | 400
17 | 410, 322 |  |  | 
18 | 411, 330 |  | 411, 330 | 
19 | 331 | 331 |  | 331

## Slide 18
n | 2→  | Intensity | Sin | Sin2 | ratio
Determination of Crystal Structure from 2 versus Intensity Data

## Slide 19
 | 2→  | Intensity | Sin | Sin2  | Simple ratio | Ratio
1 | 21.5 |  | 0.366 | 0.134 | 1 | 3
2 | 25 |  | 0.422 | 0.178 | 1.33 | 4
3 | 37 |  | 0.60 | 0.362 | 2.71 | 8
4 | 45 |  | 0.707 | 0.500 | 3.73 | 11
5 | 47 |  | 0.731 | 0.535 | 3.99 | 12
6 | 58 |  | 0.848 | 0.719 | 5.37 | 16
7 | 68 |  | 0.927 | 0.859 | 6.41 | 19
FCC

## Slide 20
h2 + k2 + l2 | SC | FCC | BCC | DC
1 | 100 |  |  | 
2 | 110 |  | 110 | 
3 | 111 | 111 |  | 111
4 | 200 | 200 | 200 | 
5 | 210 |  |  | 
6 | 211 |  | 211 | 
7 |  |  |  | 
8 | 220 | 220 | 220 | 220
9 | 300, 221 |  |  | 
10 | 310 |  | 310 | 
11 | 311 | 311 |  | 311
12 | 222 | 222 | 222 | 
13 | 320 |  |  | 
14 | 321 |  | 321 | 
15 |  |  |  | 
16 | 400 | 400 | 400 | 400
17 | 410, 322 |  |  | 
18 | 411, 330 |  | 411, 330 | 
19 | 331 | 331 |  | 331

## Slide 21
The ratio of (h2 + K2 + l2) derived from extinction rules
SC | 1 | 2 | 3 | 4 | 5 | 6 | 8 | …
BCC | 2 | 4 | 6 | 8 | 10 | 12 | 14 | …
FCC | 3 | 4 | 8 | 11 | 12 | … |  | 
DC | 3 | 8 | 11 | 16 | … |  |  | 

## Slide 22
n | 2 |  | Sin | Sin2  | ratio | Index | a (nm)
1 | 38.52 | 19.26 | 0.33 | 0.11 | 3 | 111 | 0.40448
2 | 44.76 | 22.38 | 0.38 | 0.14 | 4 | 200 | 0.40457
3 | 65.14 | 32.57 | 0.54 | 0.29 | 8 | 220 | 0.40471
4 | 78.26 | 39.13 | 0.63 | 0.40 | 11 | 311 | 0.40480
5 | 82.47 | 41.235 | 0.66 | 0.43 | 12 | 222 | 0.40480
6 | 99.11 | 49.555 | 0.76 | 0.58 | 16 | 400 | 0.40485
7 | 112.03 | 56.015 | 0.83 | 0.69 | 19 | 331 | 0.40491
8 | 116.60 | 58.3 | 0.85 | 0.72 | 20 | 420 | 0.40491
9 | 137.47 | 68.735 | 0.93 | 0.87 | 24 | 422 | 0.40494
Determination of Crystal Structure from 2 versus Intensity Data

## Slide 23
Diffraction angle (2) →
Intensity →
90
180
0
Crystal
90
180
0
Diffraction angle (2) →
Intensity →
Liquid / Amorphous solid
Schematic of difference between the diffraction patterns of various phases

## Slide 24
Crystallite size and Strain
Bragg’s equation assumes:  Crystal is perfect and infinite  Incident beam is perfectly parallel and monochromatic
Actual experimental conditions are different from these leading various kinds of deviations from Bragg’s condition  Peaks are not ‘’ curves  Peaks are broadened
There are also deviations from the assumptions involved in the generating powder patterns  Crystals may not be randomly oriented (textured sample)  Peak intensities are altered
In a powder sample if the crystallite size < 0.5 m  there are insufficient number of planes to build up a sharp diffraction pattern  peaks are broadened

## Slide 25
Instrumental
Crystallite size
Strain
Stacking fault
XRD Line Broadening
Other defects
Unresolved 1 , 2 peaks  Non-monochromaticity of the source (finite width of  peak)
Imperfect focusing
In the vicinity of B the −ve of Bragg’s equation not being satisfied
‘Residual Strain’ arising from dislocations, coherent precipitates etc. leading to broadening
In principle every defect contributes to some broadening
Bi
Bc
Bs

## Slide 26
Bravais lattice determination
Lattice parameter determination
Determination of solvus line in phase diagrams
Long range order
Applications of XRD
Crystallite size and Strain
Density ( a3 = n M / N r )

## Slide 27
Crystalline and Non-crystalline materials
Single crystal: No grain boundary
Polycrystalline: Several crystals
Anisotropy: Directionality in properties
Isotropy: No directionality

## Slide 28
An X-ray beam of wavelength 0.71 Å is diffracted by a cubic KCl crystal of density 1.99x103 Kg/m3. Calculate the interplanar spacing for (200) planes and the glancing angle for second order reflection from these planes. Mol. Wt. of KCl – 74.6 amu.
The Bragg’s angle for (220) reflection from nickel (FCC) is 38.2o when x-rays of wavelength 1.54 Å are employed in a diffraction experiment. Determine the lattice parameter of nickel.
Aluminium powder gives a diffraction pattern that yields the following eight largest d-spacings: 2.338, 2.024, 1.431, 1.221, 1.169, 1.0124, 0.9289 and 0.9055 Å. Aluminium has a cubic close packed structure and its atomic weight is 26.98 and 𝜆 = 1.5405 Å. What crystal system aluminium belongs to? Index the diffraction data.
The diffraction pattern of copper metal was measured with x-ray radiation of wavelength of 1.315Å. The first order Bragg diffraction peak was found at an angle 2θ of 50.5 degrees. Calculate the spacing between the diffracting planes in the copper metal. Index the peak.
Problems

## Slide 29
Additional Information

## Slide 30
Intensity of the Scattered electrons
Electron
Atom
Unit cell (uc)
Scattering by a crystal
A
B
C
Polarization factor
Atomic scattering factor (f)
Structure factor (F)

## Slide 31
Structure factor calculations
A
Atom at (0,0,0) and equivalent positions
 F is independent of the scattering plane (h k l)
Simple Cubic

## Slide 32
B
Atom at (0,0,0) & (½, ½, 0) and equivalent positions
 F is independent of the ‘l’ index
C- centred Orthorhombic
Real
Both even or both odd
Mixture of odd and even
e.g. (001), (110), (112); (021), (022), (023)
e.g. (100), (101), (102); (031), (032), (033)
(h + k) even
(h + k) odd

## Slide 33
Relationship between
d and lattice constant for cubic system
X
Z
Y
O
M
N
γ’
C
B
A
α’
β’

## Slide 34
From figure in a cubic lattice of
cube edge ‘a’ the intercepts of the
plane of the three axes are given by
OA = a/h
OB = a/k
OC = a/l
---- (1)

## Slide 35
Let ON = d1 = perpendicular distance from the origin
to the plane and the direction cosines of ON be
Cos α’, Cosβ’ & Cosγ’ .
Cosα’ = ON/OA = d1/a/h = d1h/a
Cosβ’ = ON/OB = d1/a/k = d1k/a
Cosγ’ = ON/OC = d1/a/l = d1l /a
--- (2)

## Slide 36
But,
Cos2α’ + cos2β’ +cos2γ’ = 1 --- (3)
Substituting eq(3) in eq(2), we get
(d1h/a)2 + (d1 k/a)2 + (d1 l/a)2 = 1
(OR)
d1 = ON = a/√h2 + k2 + l2 -- (4)

## Slide 37
Let ‘OM’ be the perpendicular distance of the next
parallel plane from the origin.
Hence, its intercepts are
OM = d1 + d1 = 2d1
= 2a/√ h2 + k2 + l2 --- (5)

## Slide 38
Therefore, the interfacing between two
adjacent planes is equal to
OM – ON = NM
Hence,
NM = 2d1 – d1 = d1
d1= a/ √h2 + k2 + l2 -----(6)
Eq(6) gives the interplanar spacing between
two adjacent parallel planes of Miller Indices.