## Slide 1: Ceramics
Dr. Ranjit Kumar
Department of Chemical Engineering
Email: ranjit.kumar@snu.edu.in

## Slide 2: Taxonomy of Ceramics
• Properties:
-- Tm for glass is moderate, but large for other ceramics.
-- Small toughness, ductility; large moduli & creep resist.
• Applications:
-- High T, wear resistant, novel uses from charge neutrality.
• Fabrication
-- some glasses can be easily formed
-- other ceramics can not be formed or cast.
Glasses
Clay
products
Refractories
Abrasives
Cements
Advanced
ceramics
-optical
-
composite
reinforce
-
containers/
household
-whiteware
-
bricks
-bricks for
high T
(furnaces)
-sandpaper
-
cutting
-
polishing
-composites
-
structural
engine
-
rotors
-
valves
-
bearings
-sensors

## Slide 3: Ceramic Bonding
• Bonding:
-- Mostly ionic, some covalent.
-- % ionic character increases with difference in
electronegativity (remember!?!).
• Large vs small ionic bond character:
SiC: small
CaF2: large

## Slide 4: Ceramic Crystal Structures
Oxide structures
  oxygen anions much larger than metal cations
  close packed oxygen in a lattice (usually FCC)
  cations in the holes of the oxygen lattice
The same ideas apply to all “ceramics”
Principles of Ceramic Architecture:
  Size relationships Cation to Anion
  Electrical Neutrality of the overall structure
  Crystallographic Arrangements
  Stoichiometry Must Match

## Slide 5: COORDINATION # AND IONIC RADII
Coordination # increases with
Issue: How many anions can you arrange around a cation?
rcation ranion
rcation ranion
Coord #
< .155
.155-.225 3
.225-.414 4
.414-.732 6
.732-1.0 8
NaCl (sodium chloride)
CsCl (cesium chloride)
ZnS (zincblende)
2

## Slide 7: Summary of Some Common Ceramic Crystal Structures

## Slide 8: Ionic Radii for Several Cations and Anions for a Coordination Number of 6

## Slide 9
Q. On the basis of ionic radii, what crystal structure do you predict for FeO?
Solution
First, note that FeO is an AX-type compound. Next, determine the cation–anion radius ratio,
This value lies between 0.414 and 0.732, and, therefore, the coordination number for the Fe2+ ion is 6; this is also the coordination number of O2− because there are equal numbers of cations and anions. The predicted crystal structure is rock salt, which is the AX crystal structure having a coordination number of 6.

## Slide 10: Practice Question
Q. the ionic radii for K+ and O2− as 0.138 and 0.140 nm, respectively.
(a) What is the coordination number for each O2− ion?
(b) Briefly describe the resulting crystal structure for K2O.
(c) Explain why this is called the antifluorite structure.

## Slide 11: Ceramic Density Computations
It is possible to compute the theoretical density of a crystalline ceramic material from unit cell data in a manner similar to metals. In this case the density 𝜌 may be determined using a modified form of Equation for metals, as follows:
where
nʹ = the number of formula units within the unit cell1
ΣAC = the sum of the atomic weights of all cations in the formula unit
ΣAA = the sum of the atomic weights of all anions in the formula unit
VC = the unit cell volume
NA = Avogadro’s number, 6.022 × 1023 formula units/mol